FLAME RETARDANTS IN PRINTED CIRCUIT BOARDS

REVIEW DRAFT

Revised

June 4, 2008

** NOT FOR DISTRIBUTION**

** DO NOT CITE OR QUOTE **

| Table ES-1 Screening Level Toxicology Hazard Summary This table only contains information regarding the inherent hazards of flame-retardant (FR) chemicals. Evaluation of risk must consider both the hazard and exposure associated with FR chemicals, as well as the hazard and exposure associated with combustion and degradation byproducts. Refer to Table 5-1 for more information on exposure. The caveats listed in the legend and footnote sections must be taken into account when interpreting the hazard information in the table below. |
| --- |
| L = Low hazard M1 = Moderate hazard H = High hazard ( Endpoints in colored text (L, M, and H) were assigned based on experimental data. Endpoints in black italics (L, M, and H) were assigned using estimated values and professional judgment (Structure Activity Relationships). ( Hazard designations, which are based on the presence of epoxy groups, arise from the analysis of low molecular weight oligomers (molecular weight <1,000) that may be present in varying amounts. The estimated human health hazards for higher molecular weight (>1,000) components, which contain epoxy groups, are low for these endpoints. ‡ Concern based on inhalation of small particles (generally less than 10 microns) that may be present in varying amounts. ( Persistent degradation products expected. R Recalcitrant: substance is or contains inorganics, such as metal ions or elemental oxides, that are expected to be found in the environment >60 days after release. |
| Chemical | CASRN | Human Health Effects | Aquatic Toxicity | Environ-mental | Exposure Considerations |
|  |  | Acute Toxicity | Skin Sensitizer | Cancer Hazard | Immunotoxicity | Reproductive | Developmental | Neurological | Systemic | Genotoxicity | Acute | Chronic | Persistence | Bioaccumulation | Availability of FRs throughout the lifecycle for reactive and additive FR chemicals and resins2 |
| Reactive Flame-Retardant Chemicals2 |
| Tetrabromobisphenol A (TBBPA) (Albemarle, Chemtura, and others) |  |
| TBBPA | 79-94-7 | L | L | L | L | L | M | L | L | L | H | H | M | L |  |
| DOPO (6H-Dibenz[c,e][1,2] oxaphosphorin, 6-oxide) (Samko Co., Ltd. and others) |  |
| DOPO | 35948-25-5 | L | L | L | L | L | L | L | L | L | M | M | L | L |  |
| Fyrol PMP (Aryl alkylphosphonate) (Supresta) |  |
| Fyrol PMP | Proprietary | L | L | L | L | L | L | L | L | L | L | L | H | L |  |
| Reactive Flame-Retardant Resins2 |
| Reaction product of TBBPA - D.E.R. 538 (Phenol, 4,4'-(1-methylethylidene)bis[2,6-dibromo-, polymer with (chloromethyl)oxirane and 4,4'-(1-methylethylidene)bis[phenol]) (Dow Chemical) |  |
| D.E.R. 538 | 26265-08-7 | L | M | M( | L | M( | M( | L | L | M | L | L | M | L |  |
| Reaction Product of DOPO – Dow XZ-92547 (reaction product of an epoxy phenyl novolak with DOPO) (Dow Chemical) |  |
| Dow XZ-92547 | Proprietary | L | M | M( | L | M( | M( | L | L | M( | L | L | H | L |  |
| Reaction product of Fyrol PMP with bisphenol A, polymer with epichlorohydrin (Representative Resin) |  |
| Representative Fyrol PCB Resin | Unknown | L | L | M( | L | M( | M( | L | L | M( | L | L | H | L |  |
| 1 The moderate designation captures a broad range of concerns for hazard, further described in Table 4-3. 2 Reactive FR chemicals and resins may not completely react, and small amounts may be available during other parts of the lifecycle. |
| L = Low hazard M1 = Moderate hazard H = High hazard ( Endpoints in colored text (L, M, and H) were assigned based on experimental data. Endpoints in black italics (L, M, or H) were assigned using estimated values and professional judgment (Structure Activity Relationships). ( Hazard designations, which are based on the presence of epoxy groups, arise from the analysis of low molecular weight oligomers (molecular weight <1,000) that may be present in varying amounts. The estimated human health hazards for higher molecular weight (>1,000) components, which contain epoxy groups, are low for these endpoints. ‡ Concern based on inhalation of small particles (generally less than 10 microns) that may be present in varying amounts. ( Persistent degradation products expected. R Recalcitrant: substance is or contains inorganics, such as metal ions or elemental oxides, that are expected to be found in the environment >60 days after release. |
| Chemical | CASRN | Human Health Effects | Aquatic Toxicity | Environ-mental | Exposure Considerations |
|  |  | Acute Toxicity | Skin Sensitizer | Cancer Hazard | Immunotoxicity | Reproductive | Developmental | Neurological | Systemic | Genotoxicity | Acute | Chronic | Persistence | Bioaccumulation | Availability of FRs throughout the lifecycle for reactive and additive FR chemicals and resins |
| Additive Flame Retardants3 |
| Aluminum hydroxide |  |
| Aluminum hydroxide | 21645-51-2 | L | L | L | M | L | L | M | L | L | H | M | HR | L |  |
| Exolit OP 930 (phosphoric acid, diethyl-, aluminum salt) (Clariant) |  |
| Exolit OP 930 | 225789-38-8 | L | L | L | M | L | M | M | L | L | M | M | HR | L |  |
| Melapur 200 (Ciba) 4 |  |
| Melapur 200 | 218768-84-4 | L | L | L | L | L | L | L | M | M | L | L | M | L |  |
| Polyphosphoric acid | 8017-16-1 | L | L | L | L | L | L | L | L | L | L | L | L | L |  |
| Melamine | 108-78-1 | L | L | L | L | L | L | L | M | M | L | L | M | L |  |
| Silicon dioxide amorphous5 |  |
| Silicon dioxide amorphous | 7631-86-9 | L | L | L | L | L | L | L | H‡ | L | L | L | HR | L |  |
| Silicon dioxide crystalline5 |  |
| Silicon dioxide crystalline | 1317-95-9 | L | L | H‡ | H‡ | L | L | L | H‡ | H‡ | L | L | HR | L |  |
| 1 The moderate designation captures a broad range of concerns for hazard, further described in Table 4-3. 3 Although additive flame retardants are present throughout the lifecycle of the PCB, they are locked into the polymer matrix of the epoxy laminate material. 4 Melapur 200 dissociates in water to form polyphosphoric acid and melamine ions. For this reason, Table 4-1 includes both dissociation ions. 5 Representative CAS numbers are included in this summary table. Section 4.2.9 includes a full list of CAS numbers. |

| Table 4-1 Screening Level Toxicology Hazard Summary This table only contains information regarding the inherent hazards of flame retardant (FR) chemicals. Evaluation of risk must consider both the hazard and exposure associated with FR chemicals, as well as the hazard and exposure associated with combustion and degradation byproducts. Refer to Table 5-1 for more information on exposure. The caveats listed in the legend and footnote sections must be taken into account when interpreting the hazard information in the table below. |
| --- |
| L = Low hazard M1 = Moderate hazard H = High hazard ( Endpoints in colored text (L, M, and H) were assigned based on experimental data. Endpoints in black italics (L, M, and H) were assigned using estimated values and professional judgment (Structure Activity Relationships). ( Hazard designations, which are based on the presence of epoxy groups, arise from the analysis of low molecular weight oligomers (molecular weight <1,000) that may be present in varying amounts. The estimated human health hazards for higher molecular weight (>1,000) components, which contain epoxy groups, are low for these endpoints. ‡ Concern based on inhalation of small particles (generally less than 10 microns) that may be present in varying amounts. ( Persistent degradation products expected. R Recalcitrant: substance is or contains inorganics, such as metal ions or elemental oxides, that are expected to be found in the environment >60 days after release. |
| Chemical | CASRN | Human Health Effects | Aquatic Toxicity | Environ-mental | Exposure Considerations |
|  |  | Acute Toxicity | Skin Sensitizer | Cancer Hazard | Immunotoxicity | Reproductive | Developmental | Neurological | Systemic | Genotoxicity | Acute | Chronic | Persistence | Bioaccumulation | Availability of FRs throughout the lifecycle for reactive and additive FR chemicals and resins2 |
| Reactive Flame Retardant Chemicals2 |
| Tetrabromobisphenol A (TBBPA) (Albemarle, Chemtura, and others) |  |
| TBBPA | 79-94-7 | L | L | L | L | L | M | L | L | L | H | H | M | L |  |
| DOPO (6H-Dibenz[c,e][1,2] oxaphosphorin, 6-oxide) (Samko Co., Ltd. and others) |  |
| DOPO | 35948-25-5 | L | L | L | L | L | L | L | L | L | M | M | L | L |  |
| Fyrol PMP (Aryl alkylphosphonate) (Supresta) |  |
| Fyrol PMP | Proprietary | L | L | L | L | L | L | L | L | L | L | L | H | L |  |
| Reactive Flame Retardant Resins2 |
| Reaction product of TBBPA - D.E.R. 538 (Phenol, 4,4'-(1-methylethylidene)bis[2,6-dibromo-, polymer with (chloromethyl)oxirane and 4,4'-(1-methylethylidene)bis[phenol]) (Dow Chemical) |  |
| D.E.R. 538 | 26265-08-7 | L | M | M( | L | M( | M( | L | L | M | L | L | M | L |  |
| Reaction Product of DOPO – Dow XZ-92547 (reaction product of an epoxy phenyl novolak with DOPO) (Dow Chemical) |  |
| Dow XZ-92547 | Proprietary | L | M | M( | L | M( | M( | L | L | M( | L | L | H | L |  |
| Reaction product of Fyrol PMP with bisphenol A, polymer with epichlorohydrin (Representative Resin) |  |
| Representative Fyrol PCB Resin | Unknown | L | L | M( | L | M( | M( | L | L | M( | L | L | H | L |  |
| 1 The moderate designation captures a broad range of concerns for hazard, further described in Table 4-3. 2 Reactive FR chemicals and resins may not completely react, and small amounts may be available during other parts of the lifecycle. |
| L = Low hazard M1 = Moderate hazard H = High hazard ( Endpoints in colored text (L, M, and H) were assigned based on experimental data. Endpoints in black italics (L, M, or H) were assigned using estimated values and professional judgment (Structure Activity Relationships). ( Hazard designations, which are based on the presence of epoxy groups, arise from the analysis of low molecular weight oligomers (molecular weight <1,000) that may be present in varying amounts. The estimated human health hazards for higher molecular weight (>1,000) components, which contain epoxy groups, are low for these endpoints. ‡ Concern based on inhalation of small particles (generally less than 10 microns) that may be present in varying amounts. ( Persistent degradation products expected. R Recalcitrant: substance is or contains inorganics, such as metal ions or elemental oxides, that are expected to be found in the environment >60 days after release. |
| Chemical | CASRN | Human Health Effects | Aquatic Toxicity | Environ-mental | Exposure Considerations |
|  |  | Acute Toxicity | Skin Sensitizer | Cancer Hazard | Immunotoxicity | Reproductive | Developmental | Neurological | Systemic | Genotoxicity | Acute | Chronic | Persistence | Bioaccumulation | Availability of FRs throughout the lifecycle for reactive and additive FR chemicals and resins |
| Additive Flame Retardants3 |
| Aluminum hydroxide |  |
| Aluminum hydroxide | 21645-51-2 | L | L | L | M | L | L | M | L | L | H | M | HR | L |  |
| Exolit OP 930 (phosphoric acid, diethyl-, aluminum salt) (Clariant) |  |
| Exolit OP 930 | 225789-38-8 | L | L | L | M | L | M | M | L | L | M | M | HR | L |  |
| Melapur 200 (Ciba) 4 |  |
| Melapur 200 | 218768-84-4 | L | L | L | L | L | L | L | M | M | L | L | M | L |  |
| Polyphosphoric acid | 8017-16-1 | L | L | L | L | L | L | L | L | L | L | L | L | L |  |
| Melamine | 108-78-1 | L | L | L | L | L | L | L | M | M | L | L | M | L |  |
| Silicon dioxide amorphous5 |  |
| Silicon dioxide amorphous | 7631-86-9 | L | L | L | L | L | L | L | H‡ | L | L | L | HR | L |  |
| Silicon dioxide crystalline5 |  |
| Silicon dioxide crystalline | 1317-95-9 | L | L | H‡ | H‡ | L | L | L | H‡ | H‡ | L | L | HR | L |  |
| 1 The moderate designation captures a broad range of concerns for hazard, further described in Table 4-3. 3 Although additive flame retardants are present throughout the lifecycle of the PCB, they are locked into the polymer matrix of the epoxy laminate material. 4 Melapur 200 dissociates in water to form polyphosphoric acid and melamine ions. For this reason, Table 4-1 includes both dissociation ions. 5 Representative CAS numbers are included in this summary table. Section 4.2.9 includes a full list of CAS numbers. |

# Text boxes

End-of-Life of Electronics (Recycle, Disposal)

Sale and Use of Electronics

Manufacture of PCB and Incorporation into Electronics

Manufacture of Laminate

Manufacture of FR Resin

Manufacture of FR

End-of-Life of Electronics (Recycle, Disposal)

Sale and Use of Electronics

Manufacture of PCB and Incorporation into Electronics

Manufacture of Laminate

Manufacture of FR Resin

Manufacture of FR

End-of-Life of Electronics (Recycle, Disposal)

Sale and Use of Electronics

Manufacture of PCB and Incorporation into Electronics

Manufacture of Laminate

Manufacture of Resin

Manufacture of FR

End-of-Life of Electronics (Recycle, Disposal)

Sale and Use of Electronics

Manufacture of PCB and Incorporation into Electronics

Manufacture of Laminate

Manufacture of Resin

Manufacture of FR

End-of-Life of Electronics (Recycle, Disposal)

Sale and Use of Electronics

Manufacture of PCB and Incorporation into Electronics

Manufacture of Laminate

Manufacture of FR Resin

Manufacture of FR

End-of-Life of Electronics (Recycle, Disposal)

Sale and Use of Electronics

Manufacture of PCB and Incorporation into Electronics

Manufacture of Laminate

Manufacture of FR Resin

Manufacture of FR